| PRODUCT NAME : EMULSIFYING WAX | EXPIRY DATE: July 2028 | LOT# : PRODUCT PACKAGE |
| --- | --- | --- |
|  | INCI: Cetearyl Alcohol (and) Polysorbate 60 |  |

| CERTIFICATE OF ANALYSIS PROPERTIES | SPECIFICATIONS | RESULTS |
| --- | --- | --- |
| APPEARANCE | WHITE WAXY SOLID GRANULES | COMPILES |
| ODOR | LITTLE INTRINSIC ODOR | COMPILES |
| SOLUBILITY | INSOULBLE IN WATER | COMPILES |
| MELTING POINT | 49 – 56 0C | 51.0 |
| ACID VALUE | <= 0.1mgKOH/g | 0.1 |
| HYDROXYLE VALUE | 215-225 mgKOH/g | 220 |
| IODINE VALUE | <= 0.50 | 0.12 |
| SAPONIFICATION VALUE | <= 1.0 mgKOH/g | 0.2 |
| CETYL ALCOHOL | 45.0 -55.0 %wt | 50.3 |
| STEARYL ACOHOL | 45.0 -55.0 %wt | 47.3 |

| STORAGE | STORE IN TIGHT CONTAINER,CLEAN , COOL, DRY PLACE AT ROOM TEMERATURE |
| --- | --- |
| SHELF LIFE | TWO YEARS IF SEALED AND STORE AWAY FROM DIRECT SUNLIGHT |