# Formulators County

CERTIFICATE OF ANALYSIS

Product Information

| Item | Description |
| --- | --- |
| PRODUCT NAME | Hydroxyethyl urea |
| PRODUCT FORM | Colorless or yellowish transparent liquid |
| PRODUCT CODE | HV-50 |
| MANUFACTURING DATE | Feb 2026 |
| LOT | BX25101501 |
| ANALYSIS DATE | Feb 2026 |
| Expiry Date | Dec 2028 |

Test Items and Results

| Item [项目] | Unit [单位] | Scope [范围] | Result [结果] |
| --- | --- | --- | --- |
| Exterior [外观] | - | Colorless/Light yellow | Colorless |
| Solid content [固含量] | % | 45-55 | 49.60 |
| PH Value [PH值] | - | 6.0-8.5 | 6.30 |
| Brookfield viscosity [布式粘度] | cps(#1,20rpm,25℃) | <200 | 7.0 |
| Packing Form [包装形式] | - | 25KG/200KG/1000KG Plastic drum/Specified | - |
| Remark [备注] | - | Shelf life: 24 months | - |
| Conclusion [结论] | - | Pass [合格] | - |

Analysis by: 	Ma Ming

Checked by: 	Wang Bo